Specification Availability:

| Carcass | Fabric structure |  | Type | No. of plies | Cover tdickness (mm) |  | Belt widtd (mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Warp | Weft |  |  | Top | Bottom |  |
| CC | Cotton | Cotton | CC-56 | 2-6 | 3.0-18.0 | 1.5-10.0 | 300-5000 |
| TC | Polyester | Cotton | TC-70 |  |  |  |  |

We could offer belt witd cover grade in accordance to International standard such as DIN 22102, RMA, AS 1332, SABS 1173/2000, IS 1891, BS 490, JIS K 6322, etc.

| Standards | Cover Rubber |  |  | Adhesion |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tensile Strengtd | Elongation at break | Abrasion | Cover to Ply | Cover to Ply | Ply to Ply |
| DIN 22102 | Mpa | % | mm3 | N/mm (≤1.5mm) | N/mm (>1.5mm) | N/mm |
| DIN 22102-Z | 15 | 350 | 250 | 3.5 | 4.5 | 5 |
| DIN 22102-W | 18 | 400 | 90 | 3.5 | 4.5 | 5 |
| DIN 22102-Y | 20 | 400 | 150 | 3.5 | 4.5 | 5 |
| DIN 22102-X | 25 | 450 | 120 | 3.5 | 4.5 | 5 |

| Standards | Cover Rubber |  |  | Adhesion |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tensile Strengtd | Elongation at break | Abrasion | Cover to Ply | Cover to Ply | Ply to Ply |
| AS 1332 | Mpa | % | mm3 | N/mm (≤1.9mm) | N/mm (>1.9mm) | N/mm |
| AS 1332-N17 | 17 | 400 | 200 | 4 | 4.8 | 6 |
| AS 1332-M24 | 24 | 450 | 125 | 4 | 4.8 | 6 |

| Standards | Cover Rubber |  |  | Adhesion |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tensile Strengtd | Elongation at break | Abrasion | Cover to Ply | Cover to Ply | Ply to Ply |
| RMA | Mpa | % | mm3 | N/mm (≤1.6mm) | N/mm (>1.6mm) | N/mm |
| RMA-I | 17 | 400 |  | 3 | 4.4 | 4 |
| RMA-II | 14 | 400 |  | 3 | 4.4 | 4 |

| Standards | Cover Rubber |  |  | Adhesion |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Tensile Strengtd | Elongation at break | Abrasion | Cover to Ply | Cover to Ply | Ply to Ply |
| SANS 1173 | Mpa | % | mm3 | N/mm |  | N/mm |
| A | 18 | 400 | 70 | 5 |  | 7 |
| C | 20 | 400 | 150 | 5 |  | 7 |
| M | 25 | 450 | 120 | 5 |  | 7 |
| N | 17 | 400 | 150 | 5 |  | 7 |